## Slide 1
Development of density functional theory for
unconventional superconductors
Ryotaro Arita
Univ. Tokyo/JST-PRESTO

## Slide 2
Outline
Materials design of high Tc superconductors
Theoretical materials design of high Tc superconductors is one of the holy grails of condensed matter theory
To achieve this goal, we need to develop a predictive method to calculate Tc

## Slide 3
Q1.
What was the most important development in your subfield in the last several years ?
A1.
Development of superconducting density functional theory (SCDFT): A predictive method to calculate Tc
Oliveira et al., PRL 60, 2430 (1988)
Kreibich & Gross PRL 86, 2984 (2001)
M. Lüders et al., PRB 72, 024545 (2005)
M. Marques et al., PRB 72, 024546 (2005)

## Slide 4
DFT for normal state
v  
Hohenberg-Kohn theorem
one-to-one correspondence
Kohn-Sham equation

## Slide 5
DFT for superconductors
electron density
anomalous density
[v,]  [,]
Hohenberg-Kohn theorem for superconductors

## Slide 6
Gap equation
Once Fxc is given, we can calculate Tc without adjustable parameters
Linearized gap equation
Exchange-correlation functional
Anomalous density

## Slide 7
Application to MgB2
 [ meV]
T [ K]
A. Floris et al, Phys. Rev. Lett. 94, 037004 (2005)

## Slide 8
Application to unconventional SC
R. Akashi and RA, PRB 88 054510 (2013)
A3C60

## Slide 9
Q2. What do you envision as the most important direction in the future for finding materials with desirable properties ?
A2.
Development of DFT for unconventional SC

## Slide 10
DFT for unconventional SC
Various mechanism of unconventional SC
• spin-fluctuation mediated SC
• orbital-fluctuation mediated SC
• exciton mechanism
• plasmon mechanism
…
R. Akashi & RA, PRL111 057006 (2013)

## Slide 11
Plasmon mechanism
Y. Takada JPSJ 45 786 (1978)
Superconducting ground state for large rs
(Low carrier density superconductor)

## Slide 12
Superconductivity in doped band insulators
Field-induced SC has been observed in a variety of band insulators
J.T. Ye et al.,
Science 338 1193 (2012)
Tc has a dope-like shape
Peak in low density region

## Slide 13
DFT for unconventional SC
Various mechanism of unconventional SC
• spin-fluctuation mediated SC
• orbital-fluctuation mediated SC
• exciton mechanism
• plasmon mechanism
…
R. Akashi & RA, PRL111 057006 (2013)

## Slide 14
Conventional SCDFT
Static screened Coulomb Vc
e-
e-
e-
e-
Phonon-mediated interaction D(w)
Energy scale ~ Debye frequency
To construct Fxc , we calculate Free energy F
For interactions between electrons in F, there are two contributions

## Slide 15
SCDFT for plasmon mechanism
Dynamical screened Coulomb Vc (w)
(using RPA)
e-
e-
e-
e-
Phonon-mediated interaction D(w)
Energy scale ~ Debye frequency
To construct Fxc , we calculate Free energy F
For interactions between electrons in F, there are two contributions
R. Akashi & RA, PRL111 057006 (2013)

## Slide 16
Li: band structure
Band structure ~ Nearly Free Electron (NFE) model

## Slide 17
High Tc SC in Li under high pressure: experiments
Shimizu et al., Nature 419, 597 (2002)
Tc~20K at 48GPa
Struzhkin et al., Science 298, 1213 (2002)
Deemyad and Schilling, PRL 91, 167001 (2003)

## Slide 18
Application to Li: Tc

## Slide 19
Application to Li: Tc
R. Akashi & RA, PRL111 057006 (2013)

## Slide 20
Q3. What do you consider the most outstanding obstacles towards designing materials starting from first principles ?
A3.
LDA-based SCDFT can not describe Mottness, Hundness → Obstacle to describe cuprates, iron-based superconductors, and go beyond

## Slide 22
Phonon contribution to Fxc
F
D
G
D
Fxca =
Fxcb =
Fxc does not have w dependence
M. Lüders et al, PRB 72, 024545 (2005)
Kohn-Sham perturbation theory

## Slide 23
F
D
Fxca =
G
D
Fxcb =
Phonon contribution to Fxc
M. Lüders et al, PRB 72, 024545 (2005)

## Slide 24
SCDFT, if Z and K=const for |e|<wD
McMillan, m*=0
N(0)Kph ~ - l
Z ~ l
so that SCDFT ~ McMillan
Comparison between SCDFT and ME

## Slide 25
Coulomb term in Migdal-Eliashberg
In Migdal-Eliashberg theory …
~EF
~wD

## Slide 26
Gap equation in SCDFT No w dependence, but state dependent
Comparison between SCDFT and ME
Kohn-Sham energy x of fi [eV]
Nb
~ wD
Zi: Diagonal part of the kernel
Damping effect (due to electron-phonon coupling) is represented

## Slide 27
Application to Li: Exch-Corr. Kernel
Fxcee =
Dynamical screened Coulomb Vc(w)

## Slide 28
Application to nitride SC
R. Akashi, K. Nakamura, RA and M. Imada PRB2012
MNX
M=Zr, Hf
X= Cl, Br, I
unconventional SC ?

## Slide 29
Plasmon mechanism
SrTiO3
Y. Takada JPSJ 49 1267 (1980)
GIC
Y. Takada JPSJ 51 63 (1982),
JPSJ 78 013703 (2009)
Cooperation of phonon & plasmon enhances pairing instability

## Slide 31
Kohn-Sham BdG equation

## Slide 32
Gap equation
Once Fxc is given, we can calculate Tc without adjustable parameters
Linearized gap equation

## Slide 33
Migdal-Eliashberg Theory
Damping and retardation effect are considered
Self-consistent perturbation theory:
lowest-order dressed-phonon and dressed Coulomb contribution to S retained
(Nambu-Gor’kov formalism)
McMillan’s formula
Can we take account of these effects in the framework of DFT ?
In DFT, everything is represented in terms of density …

## Slide 34
Diagonal part of the kernel: damping effect
Off-diagonal part of the kernel: pairing interaction
No w dependence, but state dependent
Retardation effect in SCDFT
Kohn-Sham energy x of fi [eV]
~ wD
No significant x dependence
Different x dependence
→ Retardation effect is automatically considered
Kph

## Slide 35
Application to simple metals
Transition temperatures from DFT calculation
Gap at zero temperature
M. Lüders et al, PRB 72, 024545 (2005), M. Marques et al, PRB 72, 024546 (2005)

## Slide 36
Conventional SCDFT
F (anomalous Green fn.)
D(w)
Fxce-ph =
Fxce-e =
Static screened Coulomb Vc
F (anomalous Green fn.)
Kohn-Sham perturbation theory (F, D, Vc are obtained from first-principles calc.)

## Slide 37
F (anomalous Green fn.)
D(w)
Fxce-ph =
Fxce-e =
F (anomalous Green fn.)
Dynamical screened Coulomb Vc(w)
with plasmon-pole approximation
Kohn-Sham perturbation theory (F, D, Vc are obtained from first-principles calc.)
SCDFT for plasmon mechanism

## Slide 38
F (anomalous Green fn.)
D(w)
Fxce-ph =
Fxce-e =
F (anomalous Green fn.)
Dynamical screened Coulomb Vc(w)
with plasmon-pole approximation
Kohn-Sham perturbation theory (F, D, Vc are obtained from first-principles calc.)
SCDFT for plasmon mechanism

## Slide 39
Li under high pressure: conventional scenario ?
Pressure [GPa] | 14 | 20 | 30
Ele-ph coupling (l) | 0.522 | 0.623 | 0.812
Consistent with T. Bazirov et al., PRB 82, 184509 (2010)

## Slide 40
High Tc SC in Li under high pressure: experiments
Shimizu et al., Nature 419, 597 (2002)
Tc~20K at 48GPa
(highest Tc of any elements)
Struzhkin et al., Science 298, 1213 (2002)
Deemyad and Schilling, PRL 91, 167001 (2003)

## Slide 41
Application to Li: Exch-Corr. Kernel
Fxce-e =
Dynamical screened Coulomb Vc(w)
Kohn-Sham energy x of fi [eV]

## Slide 42
Application to Li: Gap function at T=0

## Slide 43
Conventional SCDFT calc. for Li
D

## Slide 44
Application to Li: Gap function

## Slide 45
Application to Al: Tc

## Slide 46
Superconductivity in doped band insulators
K. Ueno et al.,
Nature Nanotechnology 6 408 (2011)
Field-induced SC has been observed in a variety of band insulators
J.T. Ye et al.,
Science 338 1193 (2012)
Tc has a dope-like shape
Peak in low density region

## Slide 47
Application to simple metals