## Slide 1: Electronic Delocalization in the Hunds Insulator LaMnPO: Implementing Theory Assisted Synthesis
J. W. Simonson, H. He, J. Misuraca, W. Miiller, D. McNally, A. Puri, J. Kistner-Morris, J. Hassinger, T. Orvis, S. Zellman, and M. C. Aronson
Stony Brook University and Brookhaven National Laboratory
D. Basov and K. Post Z. Yin, M. Pezzoli, and G. Kotliar
UC San Diego Rutgers University
A.Efimenko,N. Hollmann, J. Guo and L. L. Sun J. W. Allen
Z. Hu, and L. H. Tjeng CAS/IOP Beijing University of Michigan
MPI-CFS Dresden
Research supported by a DOD National Security Science
and Engineering Fellowship via the AFOSR

## Slide 2: The Materials Development Pyramid
Tier 3: Materials for Technology and Science
Improved synthesis for optimized properties
Tier 1: New Materials
Generally, only structure is known
~350,000 inorganic compounds in
ICSD/Pearsons
Tier 2: Materials of Interest
Material has special property (i.e. superconductivity)
~2,000 known
superconductors
Tier 4: Materials for real technologies and societal benefit
Material incorporated into devices and systems
<10 SCs in
Current applications
Can the combination of electronic structure calculations in synthesis speed the advancement of Tier 1 materials towards the top of the pyramid?

## Slide 3
Can Theory Speed Convergence of the Synthesis of New Materials with Specific Functionalities?
Wish to find a new family of superconductors with high SC onset temperatures: requires a new methodology
1. Need a guiding principle: (Unconventional) SC is found near the breakdown of magnetic order. High SC onset temperatures require proximity to an electronic delocalization (Mott) transition.
2. Need a structural motif: layered compounds, square net transition metals (Fe,Mn)
3. Need to verify that electronic structure calculations adequately reproduce basic quantities like charge gap, magnetic moment, etc in a prototype materials from the desired class.
Need to extrapolate electronic structure calculations to increase proximity to
desired electronic phases (electronic delocalization, collapse of moments) via doping or chemical pressure. Results must be expressed in terms of (key) atomic spacings and angles.
Need to identify Tier 1 materials from data bases that may exemplify these new properties for synthesis.

## Slide 4
Heavy Electron Intermetallics
Cuprates
AF
SC
CePd2Si2
Quantum Critical Points: A Universal Relationship for Superconductivity and Magnetism in Strongly Correlated Metals?
Mathur 1998
Organic Conductors
(Jaccard 2001)
Iron pnictides

## Slide 5: Conditions for Highest Superconducting TC ?
Hypothesis:
High superconducting transition temperatures TC are to be found on the metallic side, but close to the Mott-Hubbard (or other type of) electronic delocalization phase transition
Proximity to electronic delocalization:
enhanced Pauli susceptibility, electrical resistivity
Reduced ordered moments, kinetic energy Kmeas/Kband
Band narrowing reduces kinetic energy cost of BCS gap formation.
Kotliar and Vollhardt 2004
Qazilbash 2009

## Slide 6: Lamellar Superconductors
(LaO)(FeP) Structure
LaFePO Electronic Structure
Lebegue 2007
Functional Layers (FeP): dominate electronic states near Fermi level
Charge Reservoir Layers (LaO1-xFx): determine bandfilling.
Can we find a functional layer that is initially insulating, but can be driven metallic?

## Slide 7: Moments and Metallization: Mn Square Net Compounds
Insulating with
Magnetic Order
Metallic with
Magnetic Order
LaMnPO

## Slide 8: LaMnPO: Correlation Gap Insulator
Single crystals grown from NaCl-KCl flux: ZrCuSiAs structure
Previous measurements on polycrystalline samples (Yanagi 2009)
Optical gap: ~1 eV Resistivity: activation gap ~0.1 eV
Intrinsic insulator, localized states in gap

## Slide 9
Electronic structure calculations via DFT+DMFT
-Indirect gap (G-M, G-A) : 0.65 eV
-Direct gap (G): 0.8 eV
Total density of states in good agreement with angle integrated photoemission
experiments (Yanagi 2009, Hu and Tjeng 2011).
LaMnPO: Correlation gap insulator
DFT+DMFT
Yanagi 2009
Hu+Tjeng 2011
Gabi Kotliar, Maria Pezzoli, Zhiping Yin
Rutgers University
Liu Hao Tjeng, Zhiwei Hu, Nils Hollman, Anna Efimenko
(MPI-CFKS, Dresden), Jim Allen (U. Michigan)

## Slide 10: Antiferromagnetic Order in LaMnPO
Neutron diffraction experiments: polycrystalline material (BT-9, NIST-NCNR)
Confirm checkerboard-type magnetic structure (Yanagi 2009):
LSDA Fermi surface nestable.
Spin canting along c-axis: T*=110 K
TN=375 K, mAF(T→0) =3.2+/-0.1 mB/Mn DMFT: mAF=3.05 mB/Mn
390 K
300 K
4 K
(Yanagi 2009)

## Slide 11: Structural Evolution with Pressure in LaMnPO
Experiments carried out in diamond anvil pressure cell on Beijing Synchrotron Radiation
Facility (Beamline4W2) (L.L. Sun, J. Guo, J. Liu).
-16 GPa: transition from tetragonal ZrCuSiAs to new orthorhombic phase (c/a collapse).
-30 GPa: transition to collapsed orthorhombic phase (DV/V~ 10%).
Information needed to enforce realism of DMFT and LSDA calculations.
Pressure (GPa)
0
10
20
30
40
1 bar
c/a=2.179
Mn-P=0.1541 Ǻ
16 GPa
c/a= 1.442
Mn-P= 0.112 Ǻ
30 GPa
c/a=1.381
Mn-P= 0.0676 Ǻ
Liling Sun
Institute of Physics
Beijing

## Slide 12: Insulator-Metal Transition in LaMnPO (PC< 16 GPa)
DFT+DMFT calculations using high pressure structures: (Z. P. Yin, G. Kotliar)
Increasing valence fluctuations with increasing pressure: precursor to insulator – metal transition.
Charge gap completely suppressed for P ≤16 GPa.
1 bar
16 GPa

## Slide 13
12 GPa
19 GPa
10 GPa
17 GPa
4 GPa
9 GPa
6 GPa
Resistance measurements (hydrostatic pressure): T=0 insulator-metal transition PC=12 GPa.
LSDA: collapse of insulating gap D at 10 GPa (DMFT: D=0 for 16 GPa).
10 GPa<P<30 GPa: AF metal (Fermi liquid) with localized Mn moments (LSDA).
30 GPa: discontinuous collapse of AF Mn moment (LSDA).
DMFT
LSDA Calculations
Electronic Delocalization in Pressurized LaMnPO
Guo 2013
Simonson 2012

## Slide 14
Pressure Dependence of Optical Gap in LaMnPO
Transmission experiments carried out under hydrostatic pressures on single crystals of LaMnPO and LaMnP(O1-xFx) x=0.04 at Geophysical Laboratory of the Carnegie Institute.
Linear suppression of gap Eg with pressure: Eg→0 for P=28 GPa.
Charge gap Eg persists above insulator-metal transition: MIT from delocalization of in-gap
states.
Closure of charge gap Eg little affected by doping. PC=28 GPa (LaMnPO)
PC=26 GPa (4%F)
Post 2013

## Slide 15: Separate Metallization /Moment Collapse in LaMnPO (Uniaxial Pressure)
MIT (uniaxial pressure): 20 GPa
MIT(hydrostatic pressure): 12 GPa
TN→0: ~30 GPa (uniaxial)
Eg→0: 28 GPa
Volume collapse (XRD): ~30 GPa (hydrostatic)
Moment collapse(LSDA): ~30 Gpa (hydrostatic)
Two step delocalization transition:
-insulator-metal transition (20 GPa),
-collapse of AF order and AF moment (30 GPa), charge gap Eg (28 GPa)
Insulator-Metal transition strongly dependent on uniaxial component of pressure, while
AF collapse is not. Origin of MIT: overlap of in-gap states?
Guo 2013
Guo 2013

## Slide 16: Pressure vs Charge Doping in LaMnPO and LaMnAsO
U/W
AF-I
AF-M
PM-M
doping
LaMnPO (1 bar)
Pressure
Guo 2013

## Slide 17
A first hint of how to implement `Theory Assisted Synthesis’’
LSDA results in good agreement with D(P) for measured pressures: interpolate to determine behavior for conditions that are found in other compounds at ambient pressure.
Next steps:
-identify new starting points for materials that could be SC at 1 bar.
-in silico doping experiments: how much doping of a given type is needed to collapse gap or moment?
Predictive theory will be problematic without knowing pressure dependent structures, (in general) cannot test validity of theory without spectroscopic tools. Resource intensive: limit to generic systems (like LaMnPO).
LaMnPO
30 GPA
LaMnPO
1 bar

## Slide 18
Can Theory Speed Convergence of the Synthesis of New Materials with Specific Functionalities?
Wish to find a new family of superconductors with high SC onset temperatures: requires a new methodology.
Need a guiding principle: (Unconventional) SC is found near the breakdown of magnetic order. High SC onset temperatures require proximity to an electronic delocalization (Mott) transition.
In LaMnPO, survival of magnetic moment into metallic state may disfavor SC.
Need a structural motif: layered compounds, square net transition metals (Fe,Mn)
Many possibilities, Mn and Fe based square net compounds
Need to verify that electronic structure calculations adequately reproduce basic quantities like charge gap, magnetic moment, etc in a prototype materials from the desired class.
Good agreement with experimental D and m (1 bar, and at critical pressures)
Need to extrapolate electronic structure calculations to increase proximity to desired electronic phases (electronic delocalization, collapse of moments) via doping or chemical pressure. Results must be expressed in terms of (key) atomic spacings and angles.
Possible for current parameterizations, but may need to consider others in future.
New materials from data bases may exemplify these new properties for synthesis.





## Slide 19
Moderate Valence Fluctuations in LaMnPO
Substantial valence fluctuations from expected d5 (Mn2+) state in (La3+O2-)+(Mn2+P3-)
in DMFT histogram of states.
Valence fluctuations are weaker than in Fe-pnictides and stronger than in cuprates.
X-ray absorption measurements: not pure d5. Possible d6-ligand hole state.
LaMnPO
LaFeAsO

## Slide 20: Sizeable Exchange Component of the Charge Gap
Energy cost for electron to hop
from Mn to Mn:
on-site Coulomb interaction U
Hund’s interaction I
AF exchange energy J
With AF exchange (T<TN)
No AF exchange (kBT>SJ1)
About half of the charge gap in AF LaMnPO is due to antiferromagnetic exchange
Mn2+(d5)
Mn2+(d5)
Post 2013
D. Basov, K. Post
San Diego

## Slide 21: Robust 2-d Antiferromagnetic Correlations for T>TN
Neutron scattering experiments carried out on 13 g sample of powdered LaMnPO
using BT-7 triple axis spectrometer at the NIST Center for Neutron Research.
Antiferromagnetic correlations are limited to Mn-Mn distance for T>700 K. Defines
Effective paramagnetic limit, T>TN,MF.
Strong fluctuations due to quasi-two dimensionality of LaMnPO reduces TN from
mean field value of ~700 K to observed TN=375 K.
T=600 K
100
101

## Slide 22: Antiferromagnetic Spin Waves
Experiments on 13 g sample of powdered LaMnPO using SEQUOIA time of flight spectrometer at Spallation Neutron Source (SNS) in Oak Ridge.
Incident neutron energy Ei=250 meV. Maximum spin wave energy: ~85 meV
Two branches of dispersing spin waves centered at |Q|=1.6Å-1 (100 zone center) and 3.5 Å-1 (210 zone center).
SJ1=39 ±4 meV
S=3/2, J1=16 meV
T=5 K
T=5 K
22 meV
42 meV
62 meV

## Slide 23: S=3/2 Heisenberg Spins in LaMnPO
JC
 | LaMnPO | LaFeAsO | BaFe2As2 | CaFe2As2 | SrFe2As2
Spin Gap (meV) | 7 | 11 | 9.8 | 7 | 6.5
SJ1 (meV) | > 85 |  | 59.2 | 49.9 | < 100
J1
J2
J2/J1~ 0.3: maximum energy for spin wave density of states for SJ1~2.5
Ferromagnetic JC<<J1

## Slide 24: An Explanation for the temperature independent susceptibility
Temperature independent susceptibility: T<<J1S(S+1)/kB = Tmax ~ 560 K
Curie-Weiss susceptibility for T>Tmax.
Spin wave contribution to T=0 susceptibility: c(T=0)=0.05 J1/Ng2mB2 = 0.06879 
LaMnPO: strong deviations from mean field behavior, likely from quasi-2d
magnetic structure.
Values of J1, J2, JC all consistent with checkerboard type magnetic structure.
0
1000
500
T(K)