## Slide 1
Massimo Capone
WHEN MOTT MEETS BCS: MOLECULAR CONDUCTORS AND THE SEARCH FOR HIGH Tc SUPERCONDUCTIVITY
Massimo Capone
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 2
Massimo Capone
http://www.lemsuper.eu
http://superbadproject.wordpress.com
COWORKERS AND FUNDING
SUPERBAD
SUPERBAD
SUPERBAD
SUPERBAD
SUPERBAD
Amaricci
G. Giovannetti
A. Privitera
E. Tosatti (SISSA)
M. Fabrizio (SISSA)
C. Castellani
Toschi
G. Sangiovanni
L. de’ Medici
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 3
Massimo Capone
OUTLINE
ICAM BU Workshop – Digital Design 27-29/09/13
Cs3C60 is a Mott insulator, and it turns into a
phonon-mediated superconductor with pressure
Mott physics favours electron-phonon superconductivity
in the fullerides
Molecular phonons do not “fight” with Coulomb repulsion
Other phonons fight. Other organics?

## Slide 4
Massimo Capone
SUPERCONDUCTIVITY after the cuprate revolution
Phonon-mediated “BCS”
Weak correlations
s-wave
low Tc
Conventional
“Electronic Mechanism”
Strong Correlations
d-wave (nodes)
high Tc
Unconventional
FRAMEWORK
Cs3C60, K3C60, .. : M.C., M. Fabrizio, C. Castellani and E. Tosatti
Ba1−xKxBiO3 β-HfNCl Z. P. Yin, A. Kutepov, G. Kotliar
Aromatics?
New pieces in the puzzle (organics, iron-based, MgB2, aromatics)
[Where do the iron-based SC belong ?]
Electron-phonon superconductors which benefit from correlations
“the other high-Tcs”
Exotic, unconventional, interesting, beautiful…
Standard, conventional, boring…
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 5
SUPERBAD
SUPERCONDUCTIVITY AND MOTT PHYSICS
Main Underlying Idea
Three different families share a similar behaviour regardless of the glue:
Superconductivity is Best Realized in “Optimally Bad” Metals
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 6
Solid C60 forms a molecular crystal
Undoped Band insulator with a 3-fold degenerate (t1u, like p) LUMO
OUR NORTH START: THE FULLERIDES
Massimo Capone
A3C60: alkali-metal atoms
donate electrons to C60 bands
A = K, Rb, Cs
A=K, Rb s-wave superconductor
A=Cs AFM insulator
SC with Tc=38K at 5 kbar
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 7: THE FIRST ANSWER: ELECTRON-PHONON
Carbon Isotope effect on Tc
Regular Specific heat jump at Tc
Increase of Tc and DOS with lattice spacing
Ordinary “BCS” Superconductors with “moderate” effective mass enhancement
O. Gunnarsson, Rev. Mod. Phys. 69, 575 (1997)
Massimo Capone
“old” (90s) compounds (K3C60, Rb3C60)
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 8: THE STORY BECOMES MORE “INTERESTING”
Early 00s: Expanded (large interball distance) compounds:
Tc decreases with lattice parameter
While DOS
increases
Dahlke, Denning, Henry, Rosseinsky,
J. Am. Chem. Soc. 122, 12352 (2000)
M. Riccò et al.
Phys. Rev. B, 68, 035102 (2003)
(NH3)xNaK2C60
Cs3-xRbxC60
Massimo Capone
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 9
BACK TO THE QUESTION:
ELECTRON-PHONON OR NOT ?
Massimo Capone
Molecular Crystal: the bands are formed by molecular orbitals
C60 molecule MOs
Solid C60 bands
LUMO t1u
3 degenerate
LUMO bands
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 10: MODELING AnC60 - A “DIGITAL” PREDICTION
Coulomb Repulsion U ~ 1/1.5 eV
hopping Term
3 bands
W ~ 0.5-0.6 eV
Numbers suggest we have a correlated system
(not just Cs-doped)
Massimo Capone
One C60 per lattice site
Alkali only donate their s electrons
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 11
Electron-phonon interaction
t1u coupled to H1g phonons
(deformations of the ball)
J > 0 favors minimum S e L (inverted Hund’s rule)
Hund’s rule for t1u
MODELING AnC60 Chap. 2 - ELECTRON-PHONON
Massimo Capone
The interaction lives
on a single molecule
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 12
Orbital Degeneracy (3 t1u orbitals)
Jahn-Teller coupling
Strong Correlation
THE DMFT PHASE DIAGRAM
M. C., M. Fabrizio, C. Castellani, and E. Tosatti, Rev. Mod. Phys. 81, 943 (2009)
[before the experiment in Cs3C60]
M. C. and G. Giovannetti, Phys. Rev. Lett. 109, 166104 (2012) [HSE]
Massimo Capone
Superconductivity close to a Mott state is enhanced by correlations
s-wave superconductors
S=1/2 AFM Mott
First-order transition
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 13
ENTER Cs3C60
Massimo Capone
The “correlated” DMFT phase diagram!
A. Y. Ganin et al. Nature Materials 7, 367 (2008)
Y. Takabayashi et al., Science 323, 1585 (2009)
Cs is bigger than K, Rb
Larger lattice spacing implies a smaller W
V per C60 or U/W
S=1/2 “low spin”
ICAM BU Workshop – Digital Design 27-29/09/13
A=Cs S=1/2 AFM insulator
SC with Tc=38K at 5 kbar

## Slide 14
Coulomb Repulsion
U
ZU
Electron-phonon
J
J
W
ZW
Z << 1
M.C., M. Fabrizio, C. Castellani, and E. Tosatti, Science 296, 2364 (2002)
WHY?
Molecular phonons: deformations of the molecule which couple to
“internal” degrees of freedom.
Massimo Capone
Enhanced Superconductivity
Active Phonons are coupled with Spin/Orbital Degrees of Freedom
still active when charge fluctuations are frozen by correlations
even in the Mott state the singlet energy gain is J
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 15
l = rV
Correlations
Quasiparticles with
Reduced bandwidth
Density of States
W
ZW
Z << 1
WHAT DOESN’T KILL YOU MAKES YOU STRONGER
Attractive
Potential
Repulsion enhances Tc!
V
VZ2
r
r/ Z
l
l Z << l
“Typically”
V is also renormalized
Correlation can enhance Tc when the attraction is not renormalized
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 16
SUPERCONDUCTIVITY “HEALS”
THE ANOMALOUS METAL CLOSE
TO THE CRITICAL POINT
Superfluid delta-function
in optical conductivity
larger than the Drude
Weight of the metal
a kinetic energy gain
stabilizes the SC
Anti-BCS
(as it happens in u.d. cuprates)
WHATEVER DOES NOT KILL YOU SIMPLY
MAKES YOU STRANGER
Massimo Capone
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 17
WE MUST CONSIDER “REAL” PHONON SYMMETRY
Massimo Capone
ICAM BU Workshop – Digital Design 27-29/09/13
E-ph coupling directly “fights” with Hubbard U
(needs charge fluctuations)
Hubbard-Holstein model
Minor phonons effects, completely frozen by U
(no hope for phonon-driven superconductivity)

## Slide 18
Low energy Identical
Hubbard bands are in the same place
Phonon effects in the Hubbard bands
ICAM BU Workshop – Digital Design 27-29/09/13
Massimo Capone
STILL SOME PHONON EFFECTS
Effective Hubbard model (no phonons) vs Hubbard-Holstein

## Slide 19: AROMATIC SUPERCONDUCTORS (?)
Kx-picene
R. Mitsuhashi et al. Nature 464, 76 (2010)
2.7 < x <3.3
Tc = 18K
Kx-coronene
Tc = 15K
and 1,2:8,9-dibenzopentacene with Tc=33K
Phenanthrene
Tc = 5K
M. Xue et al. Scientific Report
X.F. Wang et al. Nat. Comm.
Y. Kubuzono et al.
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 20: PICENE MOLECULAR ORBITALS
C22H14
Y. Nomura, K. Nakamura and R. Arita, Phys. Rev. B 85, 155452 (2012)
U is around 0.7 eV
W < 0.6 eV
ICAM BU Workshop – Digital Design 27-29/09/13
Conduction bands from
LUMO and LUMO+1
nearly degenerate
T. Kosugi et al.JPSJ 79, 044705 (2010)

## Slide 21: CORRELATION EFFECTS IN K-PICENE
C22H14
G. Giovannetti and M.C. Phys. Rev. B 83, 134508 (2011); M. Kim et al.
Conduction bands from
LUMO and LUMO+1
nearly degenerate
T. Kosugi et al.JPSJ 79, 044705 (2010)
Using HSE functional within DFT we find a low-spin AFM state
No AFM using LDA, GGA – We need correlations
HSE also necessary to make Cs3C60 insulating in DFT [G. Giovannetti and M.C. PRL 2012]
AFM
Gap
Correlation effects are important
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 22: ELECTRON-PHONON AND CORRELATIONS
40% of the e-ph coupling comes from dopant+intermolecular modes
The intramolecular phonons can behave like in fullerene
The intermolecular and intercalant are expected to be depressed
Cs3C60 | K3picene
Threefold degenerate orbitals | Nearly degenerate
U/W ~ 1.5 | U/W ~ 1.2
Molecular Phonons | all sort of phonons
In-plane C
Casula et al. PRL 2011
Off-plane C
ICAM BU Workshop – Digital Design 27-29/09/13

## Slide 23: ELECTRON-PHONON AND CORRELATIONS
G. Giovannetti, M. Casula, P. Werner, M. Calandra, F. Mauri, and M.C. submitted
ICAM BU Workshop – Digital Design 27-29/09/13
Plug everything into a single phonon mode
DMFT without phonons
DMFT with phonons
METAL due to off-diagonal phonons

## Slide 24
Electron-phonon interaction and Mott physics can live happily everafter
Phononic Superconductivity favored by strong correlation if it involves internal degrees of freedom
(deformations of the molecule)
Cs3C60 is the cleanest example
The symmetry of the phonon is crucial. Need for realistic
calculations
CONCLUSIONS
M. C., M. Fabrizio, C. Castellani, and E. Tosatti, Rev. Mod. Phys. 81, 943 (2009)
Massimo Capone
G. Giovannetti and M.C. Phys. Rev. B 83, 134508 (2011)
ICAM BU Workshop – Digital Design 27-29/09/13