## Slide 1: Universal electric-field-driven resistive transition in Mott insulators and A digitally inspired prediction of novel emergent behavior in correlated materials
IMN (Nantes, France)
L. Cario
E. Janod
B. Corraze
P. Stoliar
V. Guiot
V. Ta Phuoc
C. Guillot-Deudon
S. Salmon-Bourmand
J. Tranchant
INSP (Paris, France)
T. Cren
D. Roditchev
UBA (Buenos Aires, Argentina)
C. Acha
A. Camjayi
CNEA (Buenos Aires, Argentina)
R. Weht
Marcelo Rozenberg
LPS, CNRS – Université Paris-Sud, Orsay, France
Refs:
V. Guiot et al, Nat Comm (2013)
P. Stoliar et al., Adv. Mat. (2013)

## Slide 2: The classic example: Mott transition in V2O3
McWhan et al PRB ’71 ‘73
T
pressure or chemical substitution
Equilibrium
Phase diagram

## Slide 3: AM4X8 family: « tailor-made » 3D Mott systems
A = Ga, Ge
M = V, Nb, Ta
X = S, Se
Molecular orbitals
Ueff
Energy
Gap ~ 0.20 eV
Pocha, R. et al., J. Am. Chem. Soc. 127, 8732 (2005)
4.322 Å
3.002 Å
FCC lattice of Tetrahedral Clusters
GaTa4Se8 (GTS)

## Slide 4: Metal – Insulator transition
Abd-Elmeguid et al., PRL ’04
Pressure driven Mott transition
Non Volatile Resistive Switching, t <100 ns
C. Vaju et al., Adv. Mater. ‘08
E-field driven Mott transition
Notes: In fact reported to have an insulator to metal transition driven by pressure

## Slide 5: Electric pulsing: Three different regimes
no change
RAFTER
RBEFORE
non-volatile RS
V
t
V
t
V
t
tdelay
volatile RS
GaTa4Se8 77 K
L. Cario et al. Adv. Mater. ‘10
« elastic »
« plastic »
small
medium
large
Notes: Systematic investigation of the pulsing effect

## Slide 6: Electric-field driven breakdown in GTS
V. Guiot, MR, et al. Nat Comm (2013)
Notes: Similar to electric breakdown in semiconductors

## Slide 7: Is the Mott electric-breakdown universal?
Mott
Corr Met
Three different 3D Mott-insulators: GaTa4Se8 – V2-xCrxO3 – NiS2-xSex
Mott
Corr Met
Czjzek et al JMMM ‘76

## Slide 8: Universal behavior!!
P. Stoliar, et al Adv. Mater. (2013)
Notes: Consistent with the scaling law
E_Th is much smaller than expected fro simple Hubbard model consideration

## Slide 9: What is the origin of the Mott electric-breakdown?
T. Oka et al. ‘03 ‘05 ‘10 ‘12
F. Heidrich-Meisner et al ’10
Hubbard model 1D
D ~ 10-1 eV
x ~ 1 nm = 10-7 cm
FTh ~ 1 MV/cm
ETh ~ 1 KV/cm !!!!
Notes: In fact lets consider recent work on electronic breakdown transition in Hubbard model
X No SHARP threshold effect !!!
V The threshold parameter scales like the gap^2, similar as the experiment, but not exact.
? Correlation length of doublons in 3D???

## Slide 10: 3D Mott- metal-insulator transition is well captured by the Dynamical Mean Field Theory (DMFT) of the Hubbard model
Mott
Corr Met
Czjzek et al JMMM ‘76
Mott
Corr Met
Mott
Corr Met
V2-xCrxO3 NiS2-xSex DMFT
A. Georges, G. Kotliar, MR, W. Krauth, RMP ‘96
M. Eckstein et al. ‘10 ’11 (DMFT)
A. Amaricci et al. ‘12 (DMFT)
Notes: 1D is always insulator for all U. Only doping can show a MIT
Lets focus on 3D Hubbard Mott transition

## Slide 11: DMFT of the Mott – Hubbard transition
Mott
Corr Met
U = 1
U = 2
U = 2.5
U = 3
U = 4
Mott Insulator
Corr Met
Metal
Coexistance region: 2 solutions
XY Zhang, MR, G. Kotliar, PRL ‘92
MR et al, PRL ‘95
Tcoex
Notes: Experiments are on the Ins side, well beneath the 2nd order point at low T
GTS = 77K
V2O3 = 164K
NiSeS = 4K

## Slide 12: GTS is a Mott-Hubbard insulator (exp & theory)
LDA + DMFT
A. Camjayi et el. EPJB ’12 & in preparation
C. Acha et al (in preparation)
coexistence
TCOEX = 0.025*0.25 eV
~ 70 K
Notes: GTS is physically near the coexistence region
77 K
DMFT scenario validated by LDA+DMFT calculations
Quantitatively predict the 2nd order point at about 100K
W = 0.5eV, U_MIT = 1eV, T_MIT = W/80 = 5500K/80 = 70K

## Slide 13: Model of the Mott resistive transition
Two states: MI – Mott insulator
CM – Correlated metal
RMI >> RCM
PMI->CM and PCM->MI are transition probabilities
P. Stoliar et al Adv. Mater. (2013)
Notes: Motivated by the Hubbard model results, we model the transition as a resistor network
E_CM = 20 kT
E_B = 10 kT
E_B ~ 0.01 eV
R_MI = 16
R_CM = 0.3

## Slide 14: Model results: Threshold-field Mott transition
Experiment
Theory
VS/VTh = 1.74, 1.84 1.95, 2.06

## Slide 15: How the transition evolves in time?
Each pixel is a cell of the resistor network model
Color intensity indicates the local DV drops (ie local E)

## Slide 16: Threshold effect
VS/VTh = 0.7, 1.1, 1.4, 1.8

## Slide 17: Model prediction
Model
prediction
Experiment
Transition rates imply the existence
of a relaxation time scale trelax
Short pulses (< tdelay) are sent at intervals t < trelax
Transition after 5 pulses
t

## Slide 18: Summary
E-field driven Mott insulators show a universal resistive transition with threshold behavior
A model based on DMFT Mott-Hubbard physics captures the qualitative behavior of the Mott resistive transition
Model predictions for « synaptic » behavior are validated
Refs:
V. Guiot et al, Nat Comm (2013)
P. Stoliar et al., Adv. Mat. (2013)

## Slide 19: Bulk effect => conductive path
Gold
Silver
Carbon

## Slide 20: Impact ionization, Gigantic electro-mechanical effect or small energy scale?
V. Dubost et al. Adv. Func. Mater. ’09
STM
before
after

## Slide 21: What is the Mott transition?
a correlation driven metal-insulator transition
Mott ’49
a
cannot be obtained in band theory:
not due to AF (weak coupling effect):
n
n ~ 1/a3 ~ t
t
2a


## Slide 22: E-field driven dielectric breakdown
1D Mott chains (CuO) in Sr2CuO3 and SrCuO2
Taguchi et al PRB ‘00
Notes: 1D chains
Mott-ronics and oxide electronics is now a very hot topic
Among precursors works we find Tokura’s group
At small V full gap – insulating behavior
At large V, the gap collapses as T is increased

## Slide 23: Do not mix up with the Mott transition in VO2
Zimmers et al PRL ‘13
Joule heating effect
1st order transition driven by T
E-field effect
Driscoll PRB ‘12
T
P
T
metal
insulator
met
ins
Notes: Large current activity
E field –driven Mott–transition is also mentioned in VO2
Ongoing debate by members of UC San Diego!

## Slide 24: Phenomena is generic across the AMX family E-field driven resistive transition
GaV4Se8
GaV4S8
GaNb4Se8
GeV4S8
GaTa4Se8
Notes: Robust effect

## Slide 25: Bandwidth (or gap) control by Se – Te substitution
V. Guiot et al. Nat Comm (in press)
GaTa4Se8-xTex
Notes: Systematic understanding of the E-field driven Mott transition

## Slide 26: Electric-field breakdown vs Gap
Semicond
avalanche
Mott
Eth ~ D2.5
Time delay vs Excess field
V. Guiot et al. Nat Comm (in press)
Notes: Similar to electric breakdown in semiconductors

## Slide 27: Model results: Threshold-field Mott transition
Theory
Experiment
Time delay
vs
Excess field
VS/VTh = 1.74, 1.84 1.95, 2.06

## Slide 28: What is the origin of the Mott electric-breakdown?
T. Oka et al. ‘03 ‘05 ‘10 ‘12
F. Heidrich-Meisner et al ’10
M. Eckstein et al. ‘10 ’11 (DMFT)
A. Amaricci et al. ‘12 (DMFT)
Hubbard model 1D
1/x ~ DMott (1D)
D ~ 10-1 eV
x ~ 1 nm = 10-7 cm
FTh ~ 1 MV/cm
ETh ~ 1 KV/cm !!!!
??? 1/x ~ DMott (3D)
??? x ~ mm (3D)
Notes: In fact lets consider recent work on electronic breakdown transition in Hubbard model
X No SHARP threshold effect !!!
V The threshold parameter scales like the gap^2, similar as the experiment, but not exact.
? Correlation length of doublons in 3D???

## Slide 29: What is a Mott transition?
It is a metal-insulator transition due
to electron correlation effects.
Competition between kinetic and
potential energy
Notes: Better start with recalling the basic features of the Mott transition

## Slide 30: The Hubbard model at ½ filling is a minimal model for the metal – insulator transition

metal

insulator
U = 0
t = 0

~ t

~ U
Notes: Of course out-of-equilibrium many-body problem is very difficult

## Slide 31: How the transition evolves in time? (snapshots)
time

## Slide 32: Threshold effect
Below threshold
Above threshold