## Slide 1: Understanding and Controlling the Electronic Properties of Materials with Strong Correlations
Antoine Georges
Boston University – ICAM - Sep 2013
http://www.cpht.polytechnique.fr/cpht/correl/mainpage.htm

## Slide 2: Why is the theoretically-aided design of correlated electron materials a relevant question to ask NOW ?

## Slide 3: Because a theoretical and practical framework has been emerging, which :
Takes a radically different point of view on the electronic structure of solids than the “standard model” of solid-state physics
Is not faced with the limitations of the standard model when dealing with strongly correlated systems/localized orbitals
Uses a language much closer to that of the chemist: ATOMS - atomic orbitals, bonding and hybridization (rather than Bloch bands)

## Slide 4
The standard model (most solid-state physics textbooks):
a solid is a kind of electron gas
subject to the periodic potential of ions
 Bloch wavefunctions, energy bands
Interactions complicate the matter in a somewhat annoying way
Image: K.Held
Modern (and most useful) incarnation: DFT-LDA/GGA

## Slide 5: In materials with strong correlations LOCAL ATOMIC PHYSICS is crucial

## Slide 6: The Mott Phenomenon Clear failure of the textbook picture
Note: It has NOTHING to do with magnetism. The key
is Coulomb repulsion blocking of charge motion
Electrons “hesitate: between being localized on short-time
scales and (in metals) itinerant on long time-scales

## Slide 7: Electrons “hesitate” between being localized on short-time-scales and itinerant on long time-scales
We see this from spectroscopy…

## Slide 8
Correlated metals: atomic-like excitations at
high energy, quasiparticles at low energy
- Narrowing of quasiparticle bands due to correlations (the Brinkman-Rice phenomenon)
- Hubbard satellites (i.e extension to the solid of atomic-like transitions)
Sekiyama et al., PRL 2004
SrVO3
Dashed line:
Spectrum obtained from
Conventional
band-structure methods (DFT-LDA)

## Slide 9: This is also clear from phase changes between localised and delocalised behaviour of electrons…

## Slide 10
Paramagnetic
insulator
Paramagnetic metal
Antiferromagnetic
insulator
Metal-Insulator 
Transition in V2O3
The Cerium phase
Diagram:

## Slide 11: We need to change our theoretical description and computational tools in order to deal with these « strongly-correlated electron materials »
Think in terms of atoms, not in terms of an electron gas ! [closer to a chemist point of view]
Each atom is an interacting (many-body) problem
Atomic orbitals overlap but motion of electrons is opposed by energy cost for changing the valence of each atom

## Slide 12: A theoretical description of the solid-state based on ATOMS rather than on an electron-gas picture: « Dynamical Mean-Field Theory »
Dynamical Mean-Field Theory:
A.G. & G.Kotliar, 1992
Correlated electrons in large dimensions:
W.Metzner & D.Vollhardt, 1989

## Slide 13: Dynamical Mean-Field Theory: viewing a material as an (ensemble of) atoms coupled to a self-consistent medium
Effective
Medium
Atom
Solid: crystal lattice of atoms

## Slide 14: A simple example: the Hubbard model
Focus on a given lattice site:
Atom can be in 4 possible configurations:
Describe ``history’’ of fluctuations between those configurations

## Slide 15: The happy marriage of DMFT with electronic structure (DFT) - an interdisciplinary effort started in 1996 and still continuing today Anisimov, Kotliar et al. J.Phys Cond Mat 9, 7359 (1997) (Review: Kotliar et al Rev Mod Phys 78 865, 2006)

## Slide 16: From spherical cow models… … to real materials
SrVO3
Rich interplay between: structural aspects, orbital degrees
of freedom, various intra- and inter-orbital interactions,
spin degrees of freedom, etc…

## Slide 17: Puzzle # 1: Why are 113 Vanadates Metallic while 113 Titanates are insulating ?
Interplay:
Structural distortion
Energetics of orbitals
Mott transition
Pavarini et al. PRL 92, 176403 (2004); NJP 7, 188 (2005)
See also recent work by Dang et al. arXiv:1309. 2995

## Slide 18: Vanadates and Titanates commonalities: - 1 electron in the 3d shell - Very similar values of the Hubbard U - Similar electronic structure …
SrVO3 [V4+, d1]: A metal with signatures of sizeable but moderate e-e correlations (m*/m~2.5)
CaVO3 [V4+, d1]: A metal with stronger electronic correlations (m*/m ~ 3.5)
LaTiO3 [Ti3+, d1]: A small-gap insulator (~0.2 eV)
YTiO3 [Ti3+, d1]: A larger gap insulator (~ 1eV)
WHY ?

## Slide 19: From a band-structure (DFT-LDA) point of view, they are all metals with a single electrons in t2g-like bands…
SrVO3
9=3*3
Oxygen
bands
3 V-t2g bands
2 V-eg bands
Fermi level
Pavarini et al.
PRL 92 (2004) 176403
New J.Phys 7 (2005) 188
Amadon et al.
PRB 77 (2008) 205112
Sr 5s and 4d

## Slide 20: The answer…
``It’s the bandwidth reduction,
stupid…’’
Important effect
but insufficient to
explain MIT
(U ~ 3-4 eV)

## Slide 21: Key to solving the puzzle: lifting of t2g degeneracy due to structural distortion  lowers considerably critical U
Splitting: up to 200 meV for LaTiO3, up to 330 meV for YTiO3
1 electron in:
3 degenerate orbitals, J/U=0.15  Uc/W ~ 3.5
1 single orbital  Uc/W ~ 1.5
Pavarini et al. PRL 92, 176403 (2004); NJP 7, 188 (2005)

## Slide 22: Electronic structure + Many-Body (DMFT) calculations: accouting for metallic/insulating nature of vanadates/titanates
E.Pavarini et al., PRL 2004
cf. also Sekiyama et al. (Ca/SrVO3)
PRL 2004
- Narrowing of quasiparticle bands due to correlations (the Brinkman-Rice phenomenon)
- Hubbard satellites (i.e extension to the solid of atomic-like transitions)

## Slide 23: Quantitative comparison with experiments quasiparticles + lower Hubbard band clearly resolved in bulk-sensitive photoemission experiments
Sekiyama et al,
Ca/SrVO3

## Slide 24: Strong orbital polarization predicted in the insulating materials :
LDA+DMFT calculations
(88% of d1 electron population)
(96% of d1 electron population)

## Slide 25: Puzzle # 2
Why are transition-metal oxides
of the 4d series (such as ruthenates)
strongly correlated metals, while not
being close to a Mott insulating state ?
Example: Sr2RuO4 has t2g bandwidth ~ 4eV,
And estimated U for t2g shell about 2.5 eV at most.
Nevertheless effective mass enhancement (over LDA)
of xy-band is ~ 5 !!

## Slide 26
The Platters said:
« Only U can do
make all this world
seem right… »
… Take-home message here:
« Not only U, also JH matters » !
Friedrich Hund
1896-1997

## Slide 27: Some articles of the `Hund’s metals’ saga…
Haule and Kotliar New J. Phys. 11, 025021 (2009)
Werner, Gull Troyer and Millis, PRL 101, 166405 (2008)
Mravlje et al.PRL 106, 096401 (2011)
de’Medici et al. PRL 107, 256401 (2011)
Recent review article:
AG, de’Medici and Mravlje
Annual Reviews Cond. Mat. Phys Vol 4 (2013)
arXiv:1207.3033

## Slide 28
For all filling except ½-filling and a single electron and hole:
1. Hund’s coupling suppresses coherence scale 
reduces quasiparticle coherence scale, smaller Z
2. But also increases Uc  Enhances range of metallic state !
The two faces
of Hund’s coupling

## Slide 29
J=0
J≠0

## Slide 30:  Drawing a map of early transition-metal oxides (both 3d and 4d) with Hund’s rule coupling as guidance and based on dynamical mean-field theory electronic-structure calculations

## Slide 31
3d oxides: U/D ~ 4 ; 4d oxides: U/D ~ 2
Color-intensity map of quasiparticle weight Z (~ m/m*)

## Slide 32: Puzzle # 3: record-high Néel temperature of SrTcO3 (ca. 1000K) and prediction for pressure-dependence

## Slide 33: SrTcO3 poised close to Mott transition In contrast: SrMnO3 on localized side  Prediction: distinct pressure-dep of TN

## Slide 34: Mechanism: SrTcO3 (TN~1000K) very close to Mott transition (Hund lowers Uc) (In contrast SrMnO3 is a more localized insulator, TN ~ 260 K)
Mravlje,
Aichhorn, A.G.
PRL 108, 197202
(2012)

## Slide 35: Puzzle # 4: What is the underlying critical phenomenon responsible for the “second superconducting dome” in CeCu2Si2 [not related to magnetism] ?

## Slide 36
arXiv:1305.5204 (currently in limbo at PRL…)
LDA+DMFT  Transition between two regimes dominated by different Xtal field states
``Orbital switch’’
Low-P: Xtal field energy wins, Hi-P: Hybridization wins

## Slide 37: In tetragonal environment, lowest 6-states with J=5/2 split into three doublets:
In the absence of hybridization to other electrons
(``atomic limit’’), |0> has the lowest energy.
BUT |2> has a larger hybridization to conduction electrons

## Slide 38: Level |2> has larger hybridization than |0> because it points to Si atoms

## Slide 39: As P (or T) increases, orbital switching from 0-dominated to 2-dominated
Red: 0 Blue: 2
Small/Medium/Large symbols: 7K, 14K, 58K,
Note: NOT a
crossover
such that
all Xtal field
levels are
relevant at hi-P
recovering
6-fold deg.

## Slide 40: Take-home message
We’ve come a long way in 2 decades…
Tremendous progress on materials and on experimental/instrumental techniques
Theory is coming of age: quantitative calculations become possible, with material-specific realism, and predictive capabilities
Bridging to chemistry by putting the focus on ATOMS and bonding

## Slide 41
Fundamental
Issues
Applied
challenges
cf: Donald E. Stokes
« Pasteur’s Quadrant »
Brookings Inst. Press
Condensed Matter Physics:
BOTH fundamental
AND applied
Fundamental vs. Applied Science: a false debate

## Slide 42: Let’s dream a little… CONTROLING electronic properties ? MATERIALS by design ?

## Slide 43: 1. Exploiting the sensitivity to structural degrees of freedom by strain-engineering and heterostructuring  cf. D.Schlom’s talk

## Slide 44: Oxide heterostructures: combining and controlling electronic functionalities of oxides
Hwang et al, 2002
LaTiO3/SrTiO3
Interfaces between insulators
can be conducting,
even superconducting (LAO/STO)
cf. talks on Monday: JM Triscone,…

## Slide 45: 2. Controlling these materials with LIGHT ?
cf. Andrea Cavalleri’s work

## Slide 46: A creative proposal: turning a nickelate into a superconducting cuprate-like material by strain-engineering ?
Chaloupka and Khaliullin, PRL 2008
Hansmann et al., PRL 2010
cf. Andy Millis’ talk on monday

## Slide 47
Stabilisation of the x2-y2 orbital under tensile strain
Destabilisation of the 3z2-r2 orbital
Effect enhanced by strong interactions
 Engineering a single-band material, like in cuprates or
kappa-BEDT organic materials ?

## Slide 48: Some spectacular effects have already been demonstrated…
Exciting an IR-active phonon
(up and down shaking of octahedra 71 meV ~ 17 THz)
in a manganite induces
an insulator-to-metal
Transition [Rini et al. Nature 2007]

## Slide 50: Shameless advertisement to the younger folks: Postdoc applications welcome at any time !

## Slide 51: The suspects are the localized orbitals !
* d- or f- orbitals are quite close to ions nuclei
(particularly 3d and 4f, for orthogonality reasons)
They do not behave as regular band-forming orbitals
(e.g sp-bonding) and retain atomic-like aspects
Electrons “hesitate” between
localized and itinerant behaviour !
Materials: transition-metals and their oxides, rare-earth/actinides and their compounds, but also some organic materials

## Slide 52: Layered cobaltates: cf. Lithium intercalated compounds (key materials in current batteries)
Li
LiCoO2

## Slide 53: And the saga goes on…
In his search for… transparent metals (touch-screens),
Hideo Hosono discovers in 2008 Fe-based superconductors
with quite high Tc !

## Slide 54: This description in terms of quasi-independent electrons filling up individual (Bloch) energy levels works well for many materials… but not when interactions between electrons are too strong ! (as in transition-metal oxides…)
In technical terms: Slater determinant of Bloch waves is
NOT an adequate representation of the wave-function

## Slide 55: Structural distortions: acting on both bandwidth and crystal-field splitting
Depending on the ionic radii of the 3 ions, the material often
adopts a structure which breaks perfect cubic symmetry and
can be viewed as a distorted perovskite.
Example:
`GdFeO3’ distortion
Octahedra remain perfect
(no or very small Jahn-Teller)
Rotation of octahedra along
[010] and [001]
- Orthorombic symmetry
4 M-atoms per unit cell, all
equivalent by symmetry
- M-O-M angle becomes π-θ
Other possible distortions
e.g rhomboedric, rotation [111]

## Slide 56: RMO3 : ``tolerance factor’’
- Consider close packing by hard spheres
of radii rR, rM, rO (ionic radii)
- Call a length of cubic cell
a
- Ideal packing will have:
* t=1: ideal cubic perovskite
* t<1: deforms to rhomboedral,
then orthorombic
* t too small (<0.86): unstable

## Slide 57: Effects of the orthorombic distortion on electronic structure: SrVO3, CaVO3,LaTiO3,YTiO3
Left panels: hypothetical cubic; Right panel: real structure

## Slide 58: The two effects of distortion:
1) Reduction of total t2g bandwidth:
This is because the O-M-O bond is no longer straight
 pi-bonding less efficient
2) Splitting between t2g orbitals (lifting of
orbital degeneracy)
(140,200) meV for LaTiO3 ; (200,330) meV for YTiO3
Both effects are responsible for the Mott insulating state
of LaTiO3 and YTiO3

## Slide 59: Splitting of orbital degeneracy FAVORS the transition into the Mott insulating state
Model example: 1 electron in 2 orbitals, split by Δ, J=0
(Manini et al., PRB 2002; Poteryaev et al. PRB 2008)
2-band metal
1-band metal
Fully orbital-polarized insulator
Lifting of orbital
Degeneracy:
Favors insulating state
Triggers orbital
polarization

## Slide 60: A big effort (1998-2013…): the happy marriage of DMFT with electronic structure calculations Realistic calculations with predictive power
Photoemis-sion
V2O3
Pannacionne et al. Phys Rev Lett 2006
Poteryaev et al. Phys Rev B 2007
Prediction of the phonon spectrum of
Plutonium in δ-phase
Theory: Dai et al, Science (2003);
Experiments: Wong et al

## Slide 61: Many-body Hamiltonian of a multi-orbital shell
Simple case :
well-isolated degenerate t2g triplet
in a cubic oxide
with octahedral environment of the TM atom
Kanamori hamiltonian (exact for t2g) :
See e.g.: Sugano, Tanabe & Kamimura,
Multiplets of transition-metal ions in crystals
Academic Press, 1970

## Slide 62: Another key structural degree of freedom controlling superconductivity: distance of apical oxygen from CuO2 plane

## Slide 63
Tc~ 35K
Tc~ 90K
Not entirely clear why… perhaps because of reduction
of charge-transfer energy to Ligand (Weber et al, 2011)

## Slide 64
Strain-control of apical oxygen height ?

## Slide 65: Control of screening ( electrostatic energy scales) through a tunable dielectrics (STO)

## Slide 66: Disclaimer :
Broad-brush picture
Not a technical talk
Just a very limited set of examples
Not necessarily the most recent results (rather, selected for illustrative purpose)
A somewhat idiosyncratic viewpoint (especially: emphasis on Dynamical Mean-Field Theory)

## Slide 67: Last, but not least…copper-oxide « high-Tc » superconductors
La2-xSrxCuO4
Bednorz, J.G. et K.A. Muller,
Possible high-Tc superconductivity in the Ba-La-Cu-O system.
Zeitschrift fur Physik B-Condensed. Matter, 1986
 Nobel prize, 1987
Liquid Nitrogen
Year

## Slide 68: Copper-oxide superconductors: A headache for theorists - Rich phase diagram with mysterious electronic phases
Mott Insulator
Hole injection
Electron injection
Temperature (Kelvin)
Superconducting state
Magnetic
State (AF)
« Strange » Metal
(not a conventional Fermi liquid)
Metal with
« pseudogap »

## Slide 69: The Mott phenomenon: a « toy model »
Animation: permission H.Fukuyama
Two key energy scales: t and U
t: hopping amplitude of electron between atoms
U: on-site repulsive interaction  cost of a double occupancy
Notes: Mott insulators violate this rule ! [Sir Nevil Mott, NiO]. Nobel prize. Simple explanation: this is the result of strong Coulomb interactions. Continue with cartoon picture… The packed subway Competing energy scales: t,U.

## Slide 70
U << t : A metal (itinerant state)
Band picture OK
1 electron/site  ½-filled band
U >> t An insulator
(motion blocked by repulsive interaction)
Fermi level

## Slide 71: The Mott phenomenon at strong coupling (U >> t) HAS NOTHING TO DO with magnetism It is due to blocking of density/charge
Energy scale for magnetism: superexchange J ~ t2/U
Insulating gap: ~ U > t >> J
The system is basically an insulator
even well above TNeel
Ex: MANY oxides, e.g. NiO, YTiO3, cuprates etc…
e.g. YTiO3 has a gap ~ 1eV, orders (ferro)magnetically at 30 K

## Slide 72: Beautifully illustrated by experiments on cold atoms in optical lattices with spinless bosons ! (Greiner et al. Nature, 2002)
Real-space picture: the simplest kind of insulator in nature !
[“Any 5-year old kid can understand it…Bring me a 5-year old kid ! ”
as Marx (Groucho) said]

## Slide 73: High-energy excitations of Mott insulators : atomic-like excitations reveal Coulomb energy cost
Photoemission: Fujimori et al., PRL 1992
LDA
Hubbard satellite
A Hubbard “band”
is nothing else than
an atomic transition
broadened in the
solid-state

## Slide 74: From « spherical-cow » models…
Once upon a time, in dark ages
where MaNEP did not exist,
milk production at a dairy farm was low. So the farmer asked
a condensed-matter theorist from
a nearby university for help.
After many days of intensive
calculations and scenario-building, the theorist
came back and said :
“I have the solution, but it only
works in the case of spherical
cows in vacuum…”
Exercise: in the text on the
right, replace:
`milk production  Tc’
`spherical cow
your favorite model’ …

## Slide 75
The Mott phenomenon is ubiquitous for transition-metal oxides
… but what controls it in real life ?
Atsushi Fujimori’s map of RMO3 perovskites
J.Phys Chem Sol. 53 (1992) 1595
SrVO3
CaVO3
YTiO3
LaTiO3

## Slide 76: Hund’s metals: very low scale for Fermi-Liquid behaviour and extended non-Fermi liquid crossover regime (``spin-freezing’’)
Relevant e.g. to anomalous
optics of 113 ruthenates ?
Pioneering papers:
Werner et al PRL 2008
Haule&Kotliar NJP 2009

## Slide 77: - Goal(s) of this talk – Convey enthusiasm about :
Remarkable properties of materials with strong electronic correlations
Progress in our ability to understand them theoretically over ~ 20 years, on a semi-quantitative level (while acknowledging that this is an experimentally-driven field…)
Prospects for controlling their properties and possibly for materials design

## Slide 78
Transition Metals
Rare earths and Actinides
The suspects: materials with electrons that ``hesitate’’ between being itinerant and being localized…

## Slide 79: Cobalt oxides: large Seebeck coefficient (thermopower)
Layered structure
of cobalt oxides
(after Terasaki, 2009)
Thermopower of
« misfit » cobalt oxides
(cf. Hebert, Maignan et al. CRISMAT, Caen)

## Slide 80:  Oxides for thermoelectric applications ?
Terasaki, 2009
Figure of merit ZT: need large Seebeck,
high conductivity, low thermal conductivity

## Slide 81: Some fascinating electronic properties of materials with strong electron correlations, e.g. transition-metal oxides :
- Metal-Insulator Transitions (many materials: e.g. vanadates, titanates)
High-Tc superconductivity (cuprates)
Colossal magnetoresistance (manganites)
Strong thermopower (cobaltates)
And so on…
 May be useful for something (applications)
 Fundamental questions
SOME EXAMPLES…
Notes: 1) Introduce to you some remarkable materials with remarkable electronic properties transition metal oxides - old and new ones… They do big things ! Such as: - Hi Tc superconductivity > cuprates (mention also Fe-based SC) - Hi thermopower (recall what that is…) Cobaltates - `Colossal' magnetoresistance Manganites Many more examples

## Slide 82: Fundamental question facing the theoretical description of such materials : - Electrons `hesitate’ between itinerant and localized behaviour  Descriptions in terms of electron gas and band-theory have severe limitations
Notes: 3) This mixed itinerant/localized character raises fundamental questions regarding established theoretical descriptions of the solid-state and important challenges. Indeed, conventional view of a solid: electrons form a gas ridden over the periodic potential created by ions. Almost independent electrons because strong screening of Coulomb interactions. Cartoon: a 1D chain of simplistic atoms ! Bloch waves (illustrate), Slater determinant, etc… Metals vs. insulators. e.g. one electron in one orbital > metal (more generally odd number of electrons in a shell).

## Slide 83
Hund’s J is crucial to make contact with real-life !
Back to the map of RMO3 perovskites’’…
SrVO3
CaVO3
YTiO3
LaTiO3

## Slide 84: Putting these instabilities to good use: the room-temperature MIT of Vanadium Dioxide VO2 and ``Intelligent windows’’
Hi-T rutile
structure:
~ Metal
Reflects
infra-red
Low-T
monoclinic
structure:
Insulator
Transparent
in infra-red
TMIT ~ room temperature
Cf. Tomczak & Biermann
Phys. Stat. Sol B246 (2009)

## Slide 85: Hund’s rules (1925 – Z.Phys on atomic spectra of transition metals)
Maximize S [= N/2 N<M ; = M-N/2 N>M]
Given S, maximize L
Given (S,L) lowest J=|L-S| if N<M (less than ½ filling) , highest J=L+S if N>M
N electrons in a M=2l+1-fold degenerate shell
The « bus seat rule »: better
occupy another orbital
than share one…

## Slide 86: 1. The correlating effect of the Hund’s coupling: strongly suppresses quasiparticle coherence scale known since the ~ 70’s for Kondo impurities
M.Daybell, in ‘Magnetism’ (1970); Daybell and Stayert RMP 1968; Alloul 1974

## Slide 87: 2. The decorrelating effect of the Hund’s coupling: increasing Mott critical U
cf. van der Marel&Sawatzky PRB 37 (1988) 10674 ;
L. de’ Medici PRB 83 (2011) 205112
Hund’s rule ground-state E0 not affected by spin-flip and pair-hopping terms.
N<M (N>M) :
N = M (half-filled shell) :
Max spin state only U’-J = U-3J matters
 Atomic gap and Ueff REDUCED by J for N<M, N>M
Excited state with M+1 electrons has higher energy:
 Atomic gap gap and Ueff INCREASED by J for N<M, N>M

## Slide 88: Modern formulation of electronic structure/band theory: Density-Functional Theory (DFT) and the local-density approximation (LDA) [Kohn , Hohenberg, Sham]
* Focus on local electronic density ρ(x) and
construct an energy functional:
* An exact representation of Ekin can be obtained from a one-particle
problem in an effective potential: the Kohn-Sham system
The Kohn-Sham orbitals form a reference system representing the local density
– often interpreted (at one’s own risk…) as one-electron excitation energies
* Exchange-correlation functional:
Exact form unknown. Approximation: