## Slide 1: Materials Design of Transparent Oxide Semiconductor
Hideo HOSONO
Frontier Research Center
Tokyo Institute of Technology, JAPAN
In
In2O3
In3+ 5s
STO radius

## Slide 3
e
-
2-
Edge-sharing MO6 chain
Metal vacant ns0
M+ p-block metal
TCO Frontier
Ex. In3+, Sn4+, Cd2+
Outermost
STO radius
pm
High pressure phase
( degenerate semicond.)
Nature Commun.(2011)
Sr
O
Ge
Ambient phase
(insulator)

## Slide 4: 12CaO∙7Al2O3 (C12A7)
A constituent of alumina cements
Large band gap ~7 eV
Cubic (a = 1.199 nm, I43d)
Unit cell: Ca24Al28O66 = [Ca24Al28O64]+4+ 2O2–
Unit cell
1.199 nm
Densely Packed Sub-nano-sized Cages
12 Cages
61021 cm–3
Free Oxygen Ions
11021 cm–3
Ca
Al
O
Mp. 1415 ºC
Fast Oxygen Ion Conductor
single crystal
powder
Notes: In 2003 we reported first RT stable electride using C12A7 crystal with nanoporous crstal stricture in place of organic ligands.

## Slide 5: Electronic Structure of C12A7
PRL(2003), PRB(2005), Nanolett(2007), Adv.Mat (2007)
k
-4
-2
0
2
4
6
G
X
R
Z
G
A
M
Energy (eV)
Z
Conduction Band (Framework)
Valence Band (Framework)
Cage Conduction Band
Wave functions confined in cages
O2p (Free Oxygen)
tunneling
Evac
WF=2.4eV
Notes: The small open mouse structure suppresses the invasion of O2 and H2 molecule from oitside.
Invasion
This is a energy band struture of C12A7..

## Slide 6
Metal – Insulator Transition
Hopping Conduction
Band Conduction
electron
concentration
In cages
Nc = ~1  1021 cm–3
Metal – Insulator Transition
Metal composed of typical insulators, lime and alumina !
Polaron : electron localized by lattice distortion
Nano Lett. 2007
1.5x103Scm-1@RT
3x1019cm-3
2x1021cm-3
s = ~10-10Scm-1

## Slide 7
N2 + 3H2
2NH3
Fe3O4
200-400 atm
400-600ºC
Mass production
started in 1912
Issue： Huge Energy Consumption
（1% of total energy consumed by Human Being）
Ammonia Synthesis
Harber-Bosch Process

## Slide 8
Performance
Activation Energy
black：reported
blue：C12A7:e-
Catalytic activity : ten times higher
Activation Energy : ~Half
Nat.Chem.(2012)
C12A7 electride
C12A7:O2-
N2
H2
NH3
Catalytic activity /site
Activation Energy of reaction
Cs-loaded MgO
Ba-loaded carbon
Reported

## Slide 9
Band Lineup
E
Direct
Gap
Indirect
Gap
Energy
N-type
P-type
JJAP (comprehensive review) Sep 2013
Notes: The band gap of C12A7 is ~7eV. Why can we dope electron to this material ?
The bandline up provides the reason.

## Slide 10
O2p
Sn5s - O2p
SR
APL(2008)
P-channel TFT
SnO: p-channel oxide
Phys.Stat.Sol (a) (2008)
Notes: Electronic structure of SnO.
Moderately dispersed VBM and IP is 5.8eV, rather small. The valence band top is primarily composed of Sn 5s oritals which is largely spread.
This situation is similar to n-type s-band semiconductors.
In addition, bottom of CBM is is 5eV from Evac. So, We may expect bipolarity for this material
.

## Slide 11
C-MOS inverter using two bipolar TFTs
First demonstration of C-MOS inverter
using bipolar oxide
Adv.Mater.(2011)
Notes: 第1&3象限で動差 Vthが重なっているのでVgaにならない 単極のｐ－TFTとn-TFT の組み合わせでは第一象限のみ

## Slide 12
Sr
O
Ge
O
Ge
Ambient Phase
High P Phase (>5GPa)
Cubic Perovskite
SrGeO3
Tetrahedral Ge
Octahedral Ge

## Slide 13
Electronic Structure:
Energy (eV)
Eg
CB
VB
SrGeO3
HP
AP
AP
HP
GeO2
Energy (eV)
DOS (a.u.)
Ge Sr O total
×5
×5
R  X M 
Energy (eV)
X :
M :
 :
O 2px
Ge 4s
O 2py
Eg, ind
exact
n-bonding
Bond angle
180°in c-perovskite
Nat.Commun （２０１１）
covalency &
cubic symmetry

## Slide 14
x = 0.05
x = 0.05
x = 0
x = 0
T (K)
α (μV K-1)
σ (S cm -1)
x = 0
Conductivity and Thermopower
in HP-Sr1-xLaxGeO3
Nat. Commun （２０１１）

## Slide 15
Optical Properties
ωp = 1.0 eV
τ = 2.0 fsec
Eg (Tauc) = 3.35 eV
Assumption (m*=0.3m0)
Nopt ＝2.2E20 cm-3
μopt = 12 cm2 V-1 sec-1
σopt(0) = 410 Scm-1 (bulk DC conductivity)
Drude –Tauc-Lorentz model
Eg (HP-phase) < Eg (AP-phase)

## Slide 16: Challenges
● New type of transparent metal
using abundant element
●P-type transparent semiconductors
with mobility comparable to N-type.

## Slide 18
design concept(1995)
IGZO-TFT, Science(2003)
Nature (2004)
Mass Production starts(2012)
(Nature 2002, Science 2003)
JACS 2008, Nature 2008
Ｈｉｇｈｌｉｇｈｔｓ
High Performance Transistor
Transparent Conductor
Iron Pnictide
Superconductor
molten metallic electride
( Science) 2011
Nature(1997)
Transparent
P-type oxide
Semiconductor
(CuAlO2, LaCuOCh)
2D electride
Nature(2013)
Ru
Catalyst for NH3 synthesis
(Nat.Chem.2012)

## Slide 19
CB
Cu 3d
O2p
VB
Sn 5s
O2p
(b)
O 2p
(c)
(a)
Sn 5s
O 2p
CB
Sn4+ 5s0
Sn2+ 5s2
O 2p
CB
VB
VB
N-type
P-type
P-type
(nature 1997)
(APL 2008)
P/N Orientation and Band Structure

## Slide 20
N2 + 3H2
2NH3
Fe3O4
200-400 atm
400-600ºC
Mass production
started in 1912
Issue： Huge Energy Consumption
（1% of total energy consumed by Human Being）
Ammonia Synthesis
Harber-Bosch Process

## Slide 21
Performance
Activation Energy
black：reported
blue：C12A7:e-
Catalytic activity : ten times higher
Activation Energy : ~Half
Nat.Chem.(2012)
C12A7 electride
C12A7:O2-
N2
H2
NH3
Catalytic activity /site
Activation Energy of reaction
Cs-loaded MgO
Ba-loaded carbon
Reported

## Slide 22
Glass formation
Notes: This is the phase diagram in the system of CaO and Al2O3. A classical ceramic system.
There are 5 compounds with different CaO to Al2O3 ratio. Of course, each of them is known as insulator.

## Slide 23: HAXPES spectra
Adv.Mat.(2007), JACS(2007)
Observation of CCB :Hard XPS
Sensitive to s electron
Notes: The presence of CCB can be verified by photoemission measurement. This figure shows PES of C12A7 electride usng hard X-ray from synchroron radiation.
Valence band and conduction band. You can see a distinct Fermi edge near the below the CBM.
Since the optical transition from VBM to CCB is forbidden, we cannot observed the presence of CCB by optical absorption.
So we applied HX-PES . HX PES ihas two feaatures compared with conventional XPS or UPS. First is bulk sensitive and second is s-electron sensitive.
This is an observed spectrum, We can see a clear Fermi edge between VBM and CBM and the intensity is increased with carrier concentrations.

## Slide 25: Schematic orbital Drawing
In metal
Stoichimetric
In2O3
In2O3-x
metal
radius
In3+
ionic radius
In 5s STO raduis
In3+ 5s
STO radius

## Slide 26: E-doping to C12A7
e–
TiOX
Ti
Out-diffusion of free O2-
[Ca24Al28O64]4+ (2O2–) + Ti → [Ca24Al28O64]4+ (4e–) + TiOX
cage
Free O2-
(insulating)
(metallic)
(Max 2.3x1021cm-3)
Science(2003), Nanolett(2007)
Chemical reduction
Notes: This figure shows the most efficient process to replace the free O2- ion with electrons.
That is, C12A7 crystals are sealed with metal Ti in a silica glass tube and heats it up to 1000C. The surface of C12A7 is coated with metal Ti.
When free O2- ions diffuse to the surface to react with Ti, strong Ti-O bonds are formed. As a consequence, electrons are injected to the cages to maintain electroneutrality. If this reaction proceeds 100%, the maximum concentration of 2.3x1021cm-3 should be created in the cages.