## Slide 1
Phase Change Functions in Correlated Transition Metal Oxides
Hide Takagi
Max Planck Institute for Solid State Research
Department of Physics, University of Tokyo
ICAM Boston, Sep. 27, 2013
Notes: First of all, let me thank the committee members for giving me such exciting opportunity.
Let me talk briefly about my research interest and future plan in the next half an hour.

## Slide 2
Design of phase change functions
Introduction: Concept of electronic phase
& phase change functions for electronics
2. Electronic ice pack using large entropy of correlated electrons
3. Negative thermal expansion
utilizing magneto-volume effect at phase change
with S.Niitaka (RIKEN)
with K.Takenaka(Nagoya & RIKEN)
electronic phase change can do more…
Struggle to be useful…..
Digital design
Notes: To appeal my keyword, let me first talk about the concept of electronic phase and why electronic matter interesting.
Then to help you capturing the concept,
I would like to talk about three recent works on the discovery of exotic electron matter.
Electron super-solid like phase in high-Tc cuprates
qunatum spin liquid
spin orbital electron soild
Based on those, I would like to propose department of quantum materials in Stuttgart.

## Slide 3
“Electronic matters” in TMO: a rich variety of phases associated with multiple degrees of freedom
H.Takagi & H.Y.Hwang Science 327 (2010) 1601
concept of electronic phase
charge/spin/orital almost independent
charge:solid/spin:liquid
coupling of spin-charge-orbital
even more complicated
self organized pattern of charge/spin/orital
Notes: Not only solid, liquid and gas state of electrons, in transition metal oxides, we have superfluid state, which is nothing but superconductivity and very likeky liquid crystal state. In addition, each electron has charge and spin degrees of freedom plus choice of orbitals. This multiple degrees of freedom gives rise to even richer variety of exotic phases, for example,
we can have situation where charge forms a solid, namely insulator, but spin remains liquid as we discuss lator. Analogously, we can have an orbital liquid.

## Slide 4: Exploration of novel electronic matter – goal as a basic science
20 nm
Nano-stripe formation + nano phase separation
In Ca2-xNaxCuO2Cl2
Y.Kohsaka & Takagi, Nature Phys (2012)
concept of electronic phase
Kim, Ohsumi, Arima & Takagi, Science 323, 1329 (09)
Fujiyama, Ohsumi, Arima & Takagi, PRL (12)
J1/2
J3/2
xy,yz,zx
Spin-orbital Mott state in Sr2IrO4
Quantum spin liquid state in Na4Ir3O8
Okamoto, Takagi PRL (07)
Notes: Very recently, we found nano-scale phase separation between the parent Mott insulator and the nano-stripe.
This is STM imagefor a non superconducting sample, closer to the parent insulator than the sample in the previous viewgraph..
We clearly see two fold symmetric nano stripe domains are floating on top of four fold symmetric insulating background.
Surprisingly, in nano stripe region, we still see signature of superconducting gap.
When those domains are connected, bulk superconductivity very likely emerges.
In this sense, this is a real space observation of insulator to superconductor transition.
The fact that we are able to see clear phase separation like oil and Vinegar suggests that the nano stripe is a well defined phase.

## Slide 5
Functions produced by electronic phase concept
Phase change function
Critical phase competition between more than two phases
Phase change may occur with small change of control parameters (E, B, P, T)
-> at the heart of phase change functions
- Gigantic response to external field associated with phase change: sensor
- Phase change : memory
cuprates
ruthenates
cobaltates
Rich electronic phases solid1 solid 2 , liquid 1 liquid 2 …….
competing with each other

## Slide 6
0 ≤ y ≤ 0.2, CO/OOI
“electron crystal”
0.25 ≤ y, Feromagnetic Metal
“electron liquid”
Phase change sensor & memory: controlling solid-liquid transition
B indeced M-I
-> sensor
Pr0.55(Ca1-ySry)0.45MnO3
Tomioka-Tokura
PRB(02)
Phase change electronics
E indeced M-I coupled with REDOX
-> memory
Non-volatile resistance switching memory (ReRAM)
-phase change meet with chemistry
Inoue
PRB(08)

## Slide 7
Entropic functions out of electronic phases
in transition metal oxides
H.Takagi & H.Y.Hwang Science 327 (2010) 1601
Complex, multiple degrees of freedom, highly entropic liquid
entropic electronic phase change
Phase change can do more…

## Slide 8
“10 ℃” electronic ice
Electron solid-liquid transition
in VO2 (rutile)
el. melting temperature controllable
Entropy change associated with ice-water trans.
Picnic with Wine?
ice too cold 10 ℃ ice?
shibuya et al. APL
entropic electronic phase change
El Sol,
Ins
El Liq
Met
enthalpy change/unit volume (DSC)
VO2:W (Tmelting=10 ℃)
146 J/cm3
H2O 306J/cm3
medical surgery,
raw fish…….
60 ℃ for IC chip protection

## Slide 9
Why big entropy change comparable to ice/water?
entropic electronic phase change
Contrast of entropy between high- and low- T phases
high-T: highly entropic liquid with spin & orbital degrees of freedom
low-T: low entropy solid without spin & orbital entropy
Spin entropy=Rln2 -> DH=92 J/cc << 145 J/cc @285K
all spin entropy quenched + some orbital entropy
VO2 V4+ t2g1
in the insulating state : V4+-V4+ dimer formation
spin singlet & orbital ordering
spin/orbital entropy quenched!
Notes: 9

## Slide 10
 | ΔH (J/g) | Density (g/cc) | ΔH (J/cc) | Tc (℃)
H2O | 334 | 0.917 | 306 | 0
VO2_W | 31.3 | 4.65 | 146 | 11
LiMn2O4 | 8.7 | 4.28 | 37.2 | 21
LiVS2 | 17.5 | 3.33 | 58.3 | 40
LiVO2 | 75 | 4.35 | 326 | 206
NaNiO2 | 22.5 | 4.77 | 107 | 213
Design(?) of Electronic Ice
Materials with spin singlet & orbital ordering
entropic electronic phase change
Contrast of entropy between high- and low- T phases
low-T: insulator, low entropy solid without spin & orbital entropy
Optimization: How to realize high-T, large entropy liquid?
using spin/orbital
200℃ ice

## Slide 11
Thermoelectric power
S = DV/DT = entropy / charge e
Entropic electron liquid NaCo2O4
spin/orbital entropy important
I. Terasaki, Phys. Rev. B 56, R12685 (1997).
Similar situation in LiRh2O4 Okamoto, Takagi PRL(09)
Entropic electrons for thermoelectrics
entropic electronic phase change
How to realize high-T, large entropy liquid?
NaCo2O4:SCES thermoelectrics
Notes: I have been emphasizing complexity of electronic matter.
Because of multiple degrees of freedom, electronic matter is often highly entropic.
In fact, here is a comparison of enthalpy change associated with liquid-solid transition of water and correlated electrons. As you can see, electronic matters are equally enthropic to water.
In fact, if we can demosntarte to maitain white at 11 deg, using electronic ice pack.
If we carry those electronic entropy by passing current, we can do thermoelectric conversion.
Indeed, thermoelectric power, seebeck coefficient, is nothing but entropy per electron.
based on this concept, we would like to develop novel thermoelectrics.

## Slide 12
Finding highly entropic electron liquid
S=kB/e ln x/(1-x) Heikes fomula
Configuration entropy
Koshibae, Phys. Rev. Lett. 87 (2001) 236603.
Co4+ t2g
Orbital 3 x spin 2 = 6 +DS=KB/e ln 6 ~ 150 mV/K
Enhancement due to orbital/spin
Chemist friendly approach
Digital approach
Agreement with exp.
even though SCES
Flat band (localized)
important
Localized picture OK for metal?
It works when a large S is realized.
the other way around not always true….
Arita & Kuroki,
NaCo2O4
How the band picture is connected to high-T limit picture?
Should perform 100 calcs
while we make 1 compound!
Which compound to calculate?

## Slide 13
T
T+ΔT
L0
L(T)=L0+ΔL
a(T ) = [ dL / dT ] /L
(ex. 0℃)
Some materials contract on heating
Negative Thermal Expansion (NTE)
quite useful to control or reduce “positive thermal” expansion.
mirror, stepper, resonator ,,,,,,
Strain functions out of electronic phase change
electronic phase change coupled with lattice
Phase change couples with lattice!
large magneto volume effect

## Slide 14
Magnetically frustrated anti-perovskite
Large “negative” Magneto-volume Effect in Mn3XN
J. P. Bouchaud, Anm. Chim. 3 (1968) 81.
Mn3XN (X: Zn, Ga, Ag, etc)
“only” wit non-collinear magnetic order
“frustration” matters
electronic phase change coupled with lattice
ΔL/L ～ 4×10 -3 at Tmag
Discontinuous expansion on cooling
to help spins to order
nano-disorder
300 K
Magnet-volume relaxer
In most cases, however,
no broadoning due to doping

## Slide 15
NTE α= - 20μ/K over a wide T
Isotropic and non-hysteretic
Negative Thermal Expansion with Ge-Doped Mn3XN
K. Takenaka and H. Takagi, Appl. Phys. Lett. 87 (2005) 261902
electronic phase change coupled with lattice – after the strggle with periodic table
Appl. Phys. 109 (2011) 07309. Adv. Mater. 13 (2012) 01300
【Patents】
WO2006/011590 A1
US Patent No. 7632480
CN Patent No. 200580030788.X
WO2008/081647 A1
WO2008/111285 A1
Test manufacture made from polyamideimide / NTE MnN composite
Only Ge & Sn promote volume relaxer

## Slide 16
Need for digital design
Dopant effect?
Evidences for significant local disorder induced by Ge & Sn Why?
Can we screen the effective dopant by calculation?
We spent months to find Ge and Sn
local environment by super cell approach?
Generally, dopant plays critical role in functional materials
Magneto-elastic coupling predictable?
Why large magneto-volume effect for non-colinear spins?
Can we do mining using first principle calculations?
thousands of magnets known but strain functions not known
Calculation must be much faster than synthesis!

## Slide 17
Summary
Phase change concept in correlated electron systems
brings a variety of functions
not only memory & sensor
but also
ice pack, thermoelectric, negative thermal expansion
-Digital design works better (?)